## Slide 1: Project: NMC Cathode – EXP ID: N12b CHEMISTRY: NMC811(Half) | KEY VARIABLES: NMC, EL, Loading
SPECIFICATIONS & PROTOCOL:
1. Cell & Electrode Metadata
Cathode: NMC811(BASF):PVDF:Hx-e(HCl-AW)| 94:3:3
  Loading: 7.61mg/cm2 (total); 49µm thick
  Current Collector: Al)
Electrolyte: 1M LiPF6 1:1:1, 5% FEC, 2% VC
E/C Ratio: 60µL total (4.41µL/mgactive)
Separator: CC, 2+12+2µm
2. Testing Protocol
Voltage Window: 3.0-4.2V vs. Li/Li+
Formation: 3 cycles @ C/20
Cycling Rate: C/8 Charge (CC-CV), C/8 Discharge (CC)
3. Conclusion
Active material successfully increased
Capacity could be pushed with higher cutoff voltages, assuming anode compatibility
Continue testing in full cells with leading anodes
KEY RESULTS
Metric | Benchmark | Value | Score
1st Discharge Cap. (mAh/g) | >200 | 201.3 | 
Reversible Capacity (mAh/g) | >180 | 191.4 | 
Areal Cap. (mAh/cm2) | N/A | 1.45 | 
FCE (%) | >95 | 90.14% | 
Capacity Retention(%) | >95 | 98.3% @ Cyc 20 | 
Avg. Post-Form. CE (%) | >99.9 | 99.933% |