## Slide 1
Project: NMC Cathode – EXP ID: N12b
CHEMISTRY: NMC811(Half) | KEY VARIABLES: Custom
SPECIFICATIONS & PROTOCOL:
1. Cell & Electrode Metadata
  Cathode: NMC811(BASF) (94%) | PVDF (3%) | Super P (3%)
  Loading: 7.61 mg/cm²; 49 µm thick
  Current Collector: Al
  Electrolyte: 1M LiPF6 1:1:1, 5% FEC, 2% VC
  E/C Ratio: Not recorded in DB
  Separator: CC, 2+12+2µm
2. Testing Protocol
  Voltage Window: 3.0-4.2V vs. Li/Li+
  Formation: 3 cycles
  Cycling Rate: Not recorded in DB
3. Conclusion
  Active material successfully increased.
  Capacity could be pushed with higher cutoff voltages.
KEY RESULTS
Metric | Benchmark | Value | Score
1st Discharge Cap. (mAh/g) | >200 | 201.3 | 
Reversible Capacity (mAh/g) | >180 | 191.4 | 
Areal Cap. (mAh/cm2) | N/A | 1.53 | 
FCE (%) | >95 | 90.1% | 
Capacity Retention(%) | >80 | 20 cycles | 
Avg. Post-Form. CE (%) | >99.9 | 99.9% |